Broadband MMIC Power Amplifier

for K/Ka-band Applications

Y. C. Lee and C. S. Park*

## School of Engineering, Information and Communications University

58-4 Hwaam, Yusong, Taejon 305-732, Korea

###### Abstract

A broadband MMIC power amplifier operating from 17 to 36GHz is developed for K through Ka-band applications using 0.25um AlGaAs/InGaAs/GaAs pseudomorphic high electron mobility transistor (PHEMT). The amplifier is fully monolithic, with all matching, biasing, and DC block circuitry included on the chip. The two-stage balanced power amplifier has an average gain of 11dB, maximum gain of 14dB at 31GHz, 3dB rolls-off bandwidth of 18.7GHz from 17.4GHz to 36.1GHz. At operation frequencies from 18GHz to 35GHz, output power(P1dB) was above 20dBm, and the maximum P1dB is estimated over 24dBm at 30.5GHz. The input(S11) and output(S22) return losses are less than –10dB. This power amplifier has, to our knowledge, the broadest bandwidth in the same output power level ever reported at K/Ka-band applications.

1. Introduction

Future communication services using K through Ka-band become very attractive. These services include Local Multipoint Distribution service (LMDS)[1,2] at 24.25 to 27.5GHz in Korea, at 25.35 to 28.35GHz in Canada, at around 27, 29, and 30GHz in USA, Intelligent Transport Systems (ITS) in the 24, 46, 60, and 76GHz bands, and Satellite Services in the 28, 29, and 30GHz bands. Recent studies are focused mainly on the development the MMIC power chips for these frequency bands.

The most common approach to achieve broadband gain is the negative feedback[2], distributed[3], or balanced scheme[1,4]. The negative feedback topology has a drawback of the degradation of the gain. Generally, the chip size of the distributed and balanced amplifier is large and the operating bandwidth of the distributed and balanced amplifier is limited by the bandwidth of the transmission line and the coupler[5].

In this paper, we describe the design and characteristics of a wideband MMIC power amplifier for K/Ka-band applications.

2. Power Amplifier Design

The amplifier used 0.15um x 100um and 0.15 x 200um devices as a basic cell. The first stage of power amplifier used the device with the 100um gate width to drive the second stage of the device with 200 um gate width. The PHEMT and MMIC utilize a 100-um thick GaAs substrate, through-hole via under every source for high gain and excellent thermal properties, and airbridged source interconnects.

For broadband amplifier design, balanced topology using Lange-coupler and matching network with radial stubs were used. Radial stubs are compact in size and have both a broadband behavior and well-defined low impedance levels [6,7]. The microstrip lines were added at the source terminal of the PHEMT in order to improve the transistor stability. The block diagram of the amplifier and the photograph of the fabricated MMIC power amplifier are shown in Fig. 1 and 2, respectively. The chip size of the MMIC power amplifier is 2.16mm x 2.0mm.

3. Power Amplifier Performance

The small-signal and power measurements for the MMIC power amplifier were tested on-wafer. The gain and return-loss performances of the two-stage balanced MMIC power amplifier are shown in Fig. 3. The amplifier has about 11dB of linear gain with good flatness over 17.4GHz to 36.1GHz and maximum gain of 14dB at 31GHz when biased with +5V supply. The input(S11) and output(S22) return losses are less than –10dB in these frequency bands.

Fig. 4 shows the measured output power performances as a function of input power for various frequencies. The output power at one dB compression point(P1dB) of over 20dBm is obtained. P1dB is 20dBm to 21.3dBm from 18 to 28GHz. From 30GHz to 35GHz, the power amplifier shows the linear Pin-Pout characteristics and no gain compression until Pin of 11.5dBm as shown Fig.4.

Fig.5 shows P1dB performances as a function of input frequencies of the fabricated wideband MMIC power amplifier

. At operation frequencies from 18GHz to 35GHz bands, P1dB is above 20dBm. At 30.5GHz, we can estimate the maximum P1dB of over 24dBm.

From these measured results, our study of a wideband MMIC power amplifier for 17GHz to 36GHz frequency bands is successfully achieved.

4. Summary

In this paper, a fully monolithic wideband power amplifier operating from 17 to 36GHz for K through Ka-band applications has been demonstrated. Using a 0.25um commercial AlGaAs/InGaAs/GaAs PHEMT technology, two stage balanced power amplifier achieved the small-signal gain(S21) of 11 dB and the output power at 1dB compression point of over 20dBm. The maximum P1dB is estimated over 24dBm at 30.5GHz.

Due to the broadband operation, its application can be extended to most K/Ka-band communication systems including the local multipoint distribution service (LMDS), Intelligent Transport Systems (ITS), the satellite communication, and WLAN.

# References

[1] Mansoor K. Siddiqui, et al., IEEE MTT-S Symp. Dig., (1998), P. 569~572

[2] Young-Gi Kim, et al., RAWCON’ 98 Proceedings, (1998), P.121~124.

[3] KARL. B. NICLAS, et al., IEEE Trans. Microwave Theory and Tech., Vol. MTT-31, No. 6, (1983), p.447~456

[4] Jong-Sik Lim, et al., Microwave Conference, 1999 Asia Pacific , Vol. 2 , (1999 ), P. 425 –428

[5] George D. Vendelin et al, Microwave Circuit Design, John Wiley & Son, (1990), P.253

[6 Franco Giannini et al, IEEE Trans. Mircowave Theory tech., VOL. 36, NO. 2, (1998), P. 305-313

[7] V. Sadhir, et al., Microwave Journal, August, (1991), P.102-123

# Text boxes

Fig. 4. Output power as a function of input

power for various frequencies

Fig. 5. P1dB for various frequencies

[dB]

20

10

0

-10

-20

-30

-40

40

38

36

34

32

30

28

26

24

22

20

18

16

14

12

10

Freq.[GHz]

S11

S22

S21

Fig. 3. Small-signal performances of the fabricated

wideband MMIC power amplifier

Fig. 2. Fabricated wideband MMIC power

amplifier chip (2.16X2.0mm2)

100

200

50(

50(

200

100

Fig. 1. Block diagram of wideband MMIC power amplifier